ARP® EXPANDS STAINLESS STEEL

“BULK” FASTENER LINEUP

ARP has nearly 4,500 catalog part numbers—the world’s largest selection of high performance fasteners; most of which are for specific applications. But given that there are many instances where custom components are used, ARP offers “bulk” fasteners in handy 5-packs. They are now available as small as 10-32 x ½" in length all the way up to ½" diameter by 6" length.

Made of a proprietary stainless steel alloy that’s nominally rated at 170,000 psi tensile strength, they’re much stronger than Grade 8 hardware. And they won’t rust, chip or peel like chrome plated bolts. Black oxide finished 8740 chrome moly bolts, also rated at 170,000 psi, are likewise available. Both are offered in SAE coarse, fine or Metric thread, with a choice of 12-point or hex heads.

All fasteners are manufactured in-house in ARP’s ISO 9001:2008 and AS9100 registered Southern California facilities.

The expanded lineup of “bulk” fasteners is contained in the new 2015 catalog, which is available online at www.arp-bolts.com or can be sent upon request. Technical information is available at 800-826-3045.

-30-